Purchase Description
STEEL GRIT, GRIT SIZE 40
MUST BE SAE J1993 HCS G40H.
HARDNESS MUST BE HCS G (1)H 60 HRC MINIMUM. PARTICLE SHAPE SHALL BE NO MORE THAN 5% ROUND OR HALF ROUND PARTICLES.

NO VARIATIONS OF THE DESCRIPTION WILL BE CONSIDERED.

MUST BE SHIPPED IN 50 LB BAGS.
CERTIFICATE OF ANALYSIS / MATERIAL CERTIFICATION REPORT MUST INCLUDE:
STATEMENT THAT PRODUCT MEETS SAE SPECIFICATION J1993.
MANUFACTURER NAME
PRODUCT NAME/DESCRIPTION
SPECIFICATION
 LOT/BATCH NUMBER
MANUFACTURE/EXPIRATION DATE
 ANALYTICAL DATA 
STATEMENT OF NO CHANGE IN MATERIALS OR PROCESSES
SIGNATURE OF AUTHORIZED REPRESENTATIVE

PACKAGING LABELS WILL INCLUDE:
MANUFACTURER NAME
PRODUCT NAME/DESCRIPTION
LOT/BATCH NUMBER 
MANUFACTURE/EXPIRATION DATE.





STEEL GRIT SIZE 40 DELIVERY SCHEDULE
Please deliver the following quantities on the dates below.

Delivery 1 - 40,000 lbs.
Delivery 2 - 40,000 lbs.
Delivery 3 - 40,000 lbs.
