Purchase Description

STEEL GRIT, GRIT SIZE 40

MUST BE SAE J1993 HCS G40H.

HARDNESS MUST BE HCS G (1)H 60 HRC MINIMUM. PARTICLE SHAPE SHALL BE NO MORE THAN 5% ROUND OR HALF ROUND PARTICLES.

NO VARIATIONS OF THE DESCRIPTION WILL BE CONSIDERED.

MUST BE SHIPPED IN 50 LB BAGS.
CERTIFICATE OF ANALYSIS / MATERIAL CERTIFICATION REPORT MUST INCLUDE:

STATEMENT THAT PRODUCT MEETS SAE SPECIFICATION J1993.
MANUFACTURER NAME

PRODUCT NAME/DESCRIPTION
SPECIFICATION

LOT/BATCH NUMBER

MANUFACTURE/EXPIRATION DATE

ANALYTICAL DATA

STATEMENT OF NO CHANGE IN MATERIALS OR PROCESSES

SIGNATURE OF AUTHORIZED REPRESENTATIVE

PACKAGING LABELS WILL INCLUDE:

MANUFACTURER NAME

PRODUCT NAME/DESCRIPTION

LOT/BATCH NUMBER

MANUFACTURE/EXPIRATION DATE.

STEEL GRIT SIZE 40 DELIVERY SCHEDULE
Please deliver the following quantities on the dates below.

Delivery 1 - 40,000 lbs.
Delivery 2 - 40,000 lbs.
Delivery 3 - 40,000 lbs.